Artificial intelligence-based prediction of tensile strength of 9Cr-1Mo steel printed components on the advancement of scanning strategies

Amritesh Kumar1, Shreyansh Srivastava2 Swarup Bag3*, and V C Srivastava4

1,2,3Department of Mechanical Engineering, Indian Institute of Technology Guwahati, Assam, India

4Materials Engineering Division, CSIR-National Metallurgical Laboratory, Jamshedpur, India

*Corresponding author: swarupbag@iitg.ac.in

Abstract

1 Introduction

2 Materials and methodology

Figure 1: Architecture of AI models.

Figure 2: Architectures of hybrid AI models

3 Results and discussions

Figure 3: SNS pair plot analysis.

Table 1: Anova analysis for stress

| Source | Degree of freedom | Adjusted sum of squares (x 103) | F-value (x 103) | P-value (x 10-4) | Remarks |
| --- | --- | --- | --- | --- | --- |
| Time | 1 | 1.60 | 0.0319 | 0.000162 | S |
| Extension | 1 | 7.84 | 0.157 | ~ 0 | S |
| Load | 1 | 1.47 | 2940 | 0 | S |
| I (Time ** 2) | 1 | 0.228 | 0.00456 | 328 | S |
| I (Extension ** 2) | 1 | 0.156 | 0.00311 | 777 | NS |
| I (Load ** 2) | 1 | 8.20 | 0.164 | ~ 0 | S |
| Time: Extension | 1 | 0.182 | 0.00364 | 566 | NS |
| Time: Load | 1 | 83.1 | 1.66 | 0 | S |
| Extension: Load | 1 | 81.2 | 1.62 | 0 | S |
| Residual | 22770 | 1140 |  |  |  |

Table 2: Anova analysis of strain

| Source | Degree of freedom | Adjusted sum of squares (x 10-3) | F-value (x 103) | P-value (x 10-8) | Remarks |
| --- | --- | --- | --- | --- | --- |
| Time | 1 | 106 | 3630 | 0 | S |
| Extension | 1 | 0.164 | 5.62 | 0 | S |
| Load | 1 | 0.00526 | 0.180 | ~ 0 | S |
| I (Time ** 2) | 1 | 1.80 | 61.4 | 0 | S |
| I (Extension ** 2) | 1 | 1.53 | 52.5 | 0 | S |
| I (Load ** 2) | 1 | 0.000927 | 0.0317 | 1.85 | S |
| Time: Extension | 1 | 1.67 | 0.571 | 0 | S |
| Time: Load | 1 | 0.270 | 9.21 | 0 | S |
| Extension: Load | 1 | 0.280 | 9.56 | 0 | S |
| Residual | 22770 | 0.666 |  |  |  |

Table 3: Anova analysis for models

| Error Metrics | Target | Source | Degree of freedom | Adjusted sum of squares | Adjusted mean squares | F-value | P-value |
| --- | --- | --- | --- | --- | --- | --- | --- |
| MAE | Tensile Strain | Model | 10 | 8.1598 | 0.816 | 6071.22 | P < 0.05 |
|  |  | Residual | 50105 | 6.7342 | 0.0001 |  |  |
|  |  | Total | 50115 | 14.894 |  |  |  |
|  | Tensile Stress | Model | 10 | 19824909.45 | 1982490.95 | 8715.59 | P < 0.05 |
|  |  | Residual | 50105 | 11397124.38 | 227.46 |  |  |
|  |  | Total | 50115 | 31222033.83 |  |  |  |
| MSE | Tensile Strain | Model | 10 | 0.0294 | 0.0029 | 2304.28 | P < 0.05 |
|  |  | Residual | 50105 | 0.064 | 0 |  |  |
|  |  | Total | 50115 | 0.0935 |  |  |  |
|  | Tensile Stress | Model | 10 | 1.66 x 1011 | 1.66 x 1010 | 3198.04 | P < 0.05 |
|  |  | Residual | 50105 | 2.60 x 1011 | 5184479.71 |  |  |
|  |  | Total | 50115 | 4.26 x 1011 |  |  |  |

Figure 4: Analysis of outliers present in the datasets through box plot.

Figure 5: Violin plot analysis

Figure 6: Comparison of predicted and actual stress by AI models on training and testing datasets.

Figure 7: Comparison of predicted and actual strain by AI models on training and testing datasets.

Figure 8: Actual and predicted stress-strain curve for different scan pattern using optimized models: (a) base material; (b) in-out, (c) inclined, (d) out-in, (e) longitudinal and (f) transverse.

Figure 9: Shap plot analysis for stress and strain.

Figure 10: Mean value of shap for output variable.

4 Conclusions